L20 Doors/ Shutters/ Hatches

610 Roller shutter doors 

Specification Text 

Manufacturer: HVP Security Shutters Ltd, 4 Grace Road West, Marsh Barton, Exeter, EX2 8PU. Tel: 01392 270 218. Fax: 01392 278 548. Email: info@hvpshutters.co.uk Website: www.hvpshutters.co.uk. 

Product reference: Barricade Collapsible Gate.

Arrangement: Sideway folding collapsible gate, to be fitted within or around the reveal.
Construction: Manufactured from all galvanised high grade steel and supplied in 'X' lattice as standard or 'S' lattice as an option. 
Top hung on nylon coated steel bearings. Overlapped locking profiles. Optional folding bottom track. Optional hinge aside (non-insurance rated version only). Strong steel lattice with smooth durable finish. Steel riveted lattice assembly system.
Finish as delivered: Powder coated pre-galvanised steel. 
Operation: Manual operation.

Locking Options: Two point locking (four point for the insurance approved version) from a single key with the lock mechanism shielded by a steel plate.
Weight and Stacking: 19kgm2 nominal. An unlimited width can be accommodated with multiple sashes. Sashes to be made in single pieces up to 2m wide. Larger sizes to be made in sections for assembly on site, ensuring the weight of each section can be handled safely. Gates wider than 4m will to be supplied with the top track in two pieces, the split to be in the middle. Where two split sashes meet two pickets are joined together using bolts and fixing plates. 
Insurance approved version (optional): As above with the following changes: 

· Lattice assembly system to utilise high grade steel screws; 

· Gate to be independently tested and approved to Loss Prevention Standard (LPS) 1175 Security Rating Classification 1;

· Gate to carry the LPCB mark on a metal plate fixed to the outside of the product;

· Gate to be installed in accordance with the requirements of LPS 1175, as per below: 

· Minimum fixing distance from edge of reveal : 50mm.

· Maximum fixing distance from any corner : 100mm.

· Maximum distance between fixing : 400mm.
· All fixing heads spoiled:

· Masonry: 2.5” x 12s   
· Wood: 4.0” x 12s   
· Steel: 1.0” x M8s   
Other requirements:
